{}

$

Effectiveness of chitosan nanohydrogel mediated encapsulation of EcR dsRNA against the whitefly, Bemisia tabaci Asia-I

- Source: Pesticide Biochemistry and Physiology 2024

- DOI: 10.1016/j.pestbp.2023.105712

- Scope: Formulation, stability, and bioefficacy testing of chitosan nanoparticle hydrogel (CNP) for dsRNA oral delivery in whiteflies.

- Study_type: functional knockdown, nanocarrier formulation, dsRNA stability

- Target_context: RNAi-mediated pest management via nanoparticle-protected dsRNA

- Organism_or_system: Bemisia tabaci (Asia-I, Hemiptera: Aleyrodidae)

- Delivery_or_intervention_mode: oral feeding via artificial diet (encapsulated dsRNA)

$

Metadata

Source: Pesticide Biochemistry and Physiology 2024

DOI: 10.1016/j.pestbp.2023.105712

Scope: Developing and validating a chitosan nanoparticle hydrogel (CNP) as a protective carrier for dsRNA to enhance RNAi efficacy in whiteflies via oral delivery.

Study_type: Formulation and bioassay

Organism: Bemisia tabaci (Asia-I)

Developmental_stage: Adult

Delivery_mode: Oral feeding

Molecule_or_intervention_type: dsRNA targeting Ecdysone Receptor (EcR) gene, encapsulated in chitosan nanohydrogel (CNP)

Application_context: Laboratory bioassay

Validation_level: multi-level (molecular knockdown confirmation via qRT-PCR, phenotypic mortality)

Target_gene_or_pathway: Ecdysone Receptor (EcR)

$

Usage note

This document is intended for experimental workflow guidance and protocol-level reasoning.

Numerical parameters and optimization details should be adapted to specific experimental contexts.

{}

$

Sub-protocol 1: Whitefly Rearing for Bioassay

**[PROTOCOL_STAGE=ORGANISM_REARING]**

$

Applicable when:

Establishing a continuous, controlled colony of Bemisia tabaci (Asia-I biotype) for use in dsRNA bioassays.

$

Purpose:

To provide a standardized, healthy population of target insects of defined age and physiological state for consistent experimental feeding assays.

$

Procedure:

1.  Maintain brinjal (Solanum melongena cv. Arka Keshav) seedlings as host plants in 10 kg sand pots with a 1:1 potting mix of farm yard manure and red soil.

2.  Initiate colony with field-collected adult whiteflies using an aspirator. Release them onto healthy brinjal plants within a polyhouse.

3.  Rearing: Maintain the whiteflies continuously for multiple generations inside an insect-proof cage (60.96 x 76.2 x 91.44 cm).

4.  Environmental Control: Maintain conditions at 25-26 °C, 65 ± 5% relative humidity, and a 15:9 hour (Light:Dark) photoperiod.

5.  Host Plant Stage: Use brinjal plants at the five to eight-leaf stage for rearing.

6.  Bioassay Preparation: For bioassays, collect and use one-day-old freshly hatched adult whiteflies.

$

Key materials and equipment:

- Host plant: Brinjal (Solanum melongena cv. Arka Keshav)

- Rearing cage (insect-proof, 60.96" x 76.2" x 91.44")

- Environmental chamber or controlled room (temp, humidity, photoperiod)

- Aspirator

$

Controls_and_validation:

Colony is validated by continuous, healthy propagation over multiple generations.

$

Notes

Ensure the colony is free from pathogens and maintained under strict environmental control to minimize phenotypic variability. Plants should be at a consistent growth stage.

{}

$

Sub-protocol 2: In vitro Synthesis and Purification of Target dsRNA

**[PROTOCOL_STAGE=DSRNA_SYNTHESIS]**

$

Applicable when:

Producing specific dsRNA targeting a gene of interest (EcR) for RNAi experiments.

$

Purpose:

To generate high-purity, intact dsRNA molecules from a DNA template for downstream encapsulation and bioassay.

$

Procedure:

1.  Template Preparation: Amplify the target gene fragment (EcR) by PCR using a forward primer containing the T7 promoter sequence.

2.  In vitro Transcription: Synthesize dsRNA using the PCR product as a template and T7 RNA polymerase (e.g., Thermo Scientific).

3.  DNase Treatment: Treat the synthesized dsRNA with DNase I (e.g., Thermo Scientific) to remove DNA template.

4.  Purification: Purify the dsRNA using Phenol:Chloroform extraction followed by ethanol precipitation.

5.  Quality Control:

a.  Quantify concentration using a spectrophotometer (e.g., NanoDrop 2000).

b.  Assess integrity by running an aliquot on an agarose gel.

6.  Storage: Store purified dsRNA at -20 °C until use.

$

Key materials and equipment:

- T7 RNA Polymerase kit (Thermo Scientific)

- DNase I (Thermo Scientific)

- Phenol:Chloroform, Ethanol

- NanoDrop 2000 spectrophotometer

- Agarose gel electrophoresis system

$

Controls_and_validation:

PCR product and dsRNA integrity are validated via agarose gel electrophoresis. Concentration is quantified spectrophotometrically.

$

Notes

Primer design must include T7 promoter sequence. All steps should be performed RNase-free to prevent degradation. Gel electrophoresis confirms the absence of degradation (smearing) and the presence of a single, sharp band.

{}

$

Sub-protocol 3: Preparation of Chitosan Nanohydrogel (CNP) Stock

**[PROTOCOL_STAGE=FORMULATION_PREPARATION]**

$

Applicable when:

Preparing a biocompatible, nanoparticle-forming hydrogel using chitosan and glycerol without chemical crosslinkers.

$

Purpose:

To create a biopolymer nanoparticle stock solution that can later be complexed with dsRNA for encapsulation and protection.

$

Procedure:

1.  Solution Preparation: Mix 1 gram of chitosan biopolymer (MW 3800–20,000 Da, ≥75% deacetylation) with 100 ml of glycerol (85–88% purity) in a w/v ratio.

2.  Homogenization: Heat the mixture at 60 °C with constant stirring for 30 minutes until a homogeneous mixture is achieved.

3.  Cooling: Cool the mixture down to room temperature.

4.  Gelation: Store the colloidal hydrogel at -4 °C overnight to complete the gel formation process (freeze-thaw method). This is the 1% chitosan nanohydrogel stock.

$

Key materials and equipment:

- Chitosan biopolymer (specified MW and deacetylation)

- Glycerol (high purity)

- Heating stir plate

- Storage at -4 °C

$

Controls_and_validation:

Formation of a homogeneous, colloidal stock solution is the primary validation.

$

Notes

This method uses a physical freeze-thaw process, avoiding toxic crosslinking agents. The quality of starting chitosan (MW, deacetylation %) is critical for consistent nanoparticle formation.

{}

$

Sub-protocol 4: Formulation of dsRNA-CNP Complex (Encapsulation)

**[PROTOCOL_STAGE=FORMULATION_PREPARATION]**

$

Applicable when:

Loading dsRNA onto/into chitosan nanohydrogel nanoparticles to form a protective complex for oral delivery.

$

Purpose:

To physically complex dsRNA with chitosan nanoparticles, facilitating encapsulation, protection from degradation, and potentially enhancing cellular uptake.

$

Procedure:

1.  Ratio Testing: Formulate complexes at various CNP:dsRNA volume ratios (e.g., 100:1, 150:1, 200:1, 250:1). A common loading is 2 μg of dsRNA per formulation.

2.  Mixing: Vortex the mixture of CNP stock and dsRNA for five minutes.

3.  Sonication: Sonicate the mixture for 30 minutes at 37 °C.

4.  Incubation: Keep the dsRNA-loaded hydrogel samples overnight at -20 °C to enhance encapsulation efficiency.

5.  Validation (Gel Retardation Assay): Confirm successful complexation/binding by running the complex on a 1% agarose gel. Free dsRNA migrates, while complexed dsRNA is retained in the well.

$

Key materials and equipment:

- Chitosan nanohydrogel (CNP) stock

- Purified dsRNA

- Vortex mixer

- Sonicator (maintaining 37 °C)

- Agarose gel electrophoresis system

$

Controls_and_validation:

Gel retardation assay: Naked dsRNA (migrates) serves as a positive control, non-conjugated hydrogel (no band) as a negative control. Successful complexation shows dsRNA retained in well.

$

Notes

The optimal ratio (e.g., 200:1 v/v) must be determined empirically via gel retardation and subsequent bioassay. Sonication temperature and time are critical for nanoparticle formation and loading.

{}

$

Sub-protocol 5: Characterization of CNP/dsRNA Complex (Morphology & Confirmation)

**[PROTOCOL_STAGE=FORMULATION_PREPARATION]**

$

Applicable when:

Physically characterizing the formulated nanoparticle-dsRNA complex to confirm size, shape, and successful incorporation of dsRNA.

$

Purpose:

To provide evidence of nanoparticle formation, dsRNA interaction, and to characterize the physical properties of the delivery complex.

$

Procedure:

1.  FE-SEM (Field Emission Scanning Electron Microscopy):

a.  Apply 30 μL of dried sample (CNP or CNP/dsRNA) on a Copper (Cu) grid (coated for conductivity).

b.  Analyze shape and surface texture using FE-SEM.

2.  HR-TEM (High Resolution Transmission Electron Microscopy):

a.  Dissolve CNP/dsRNA nanoparticles in water, vortex for 5 minutes.

b.  Incubate a droplet on a grid at room temperature for 10 min to dry.

c.  View morphology under TEM and analyze images with software (e.g., ImageJ).

3.  FTIR (Fourier Transform Infrared Spectroscopy):

a.  Analyze samples (CNP, dsRNA, CNP/dsRNA) in the range of 4000 - 400 cm⁻¹ using the KBr method or ATR (Attenuated Total Reflectance).

b.  Identify functional groups and confirm interactions/shifts indicating dsRNA encapsulation.

$

Key materials and equipment:

- Field Emission Scanning Electron Microscope (FE-SEM)

- High Resolution Transmission Electron Microscope (HR-TEM)

- Fourier Transform Infrared Spectrometer (FTIR)

- Copper grids

- ImageJ software

$

Controls_and_validation:

Compare CNP alone vs. CNP/dsRNA complex. FTIR shifts indicate interaction. Microscopy confirms nanoparticle formation and any morphological changes post-loading.

$

Notes

These are characterization steps, not part of routine bioassay preparation. They are used for initial formulation validation and publication.

{}

$

Sub-protocol 6: Stability Assessment of CNP/dsRNA Complex

**[PROTOCOL_STAGE=FORMULATION_PREPARATION]**

$

Applicable when:

Testing the protective capacity of the chitosan nanohydrogel against environmental degradation factors relevant to field application (sunlight, UV, heat).

$

Purpose:

To evaluate if the CNP formulation enhances the durability of dsRNA compared to naked dsRNA under stressful conditions.

$

Procedure:

1.  Sample Preparation: Prepare samples of naked dsRNA and CNP/dsRNA complex in aqueous solution.

2.  Light Exposure Test:

a.  Place 50 μL of each sample in an open glass petri dish (60 x 15 mm).

b.  Expose separately to direct sunlight and to an ultraviolet (UV) light source.

c.  Collect samples at time points: 0, 1, 2, 4, 6, and 8 hours.

3.  Heat Incubation Test:

a.  Place naked dsRNA and CNP/dsRNA samples (in 500 μL tubes) in a water bath at 37 °C.

b.  Collect samples at different time periods: 0, 1, 2, 4, 6, 8, and 12 hours, and also on different days (24, 48, and 72 hours).

4.  Analysis: After exposure/incubation, mix all collected samples with loading dye and analyze integrity via 1% agarose gel electrophoresis.

$

Key materials and equipment:

- UV light source

- Water bath (37 °C)

- Glass petri dishes

- Agarose gel electrophoresis system

$

Controls_and_validation:

Naked dsRNA serves as the degradation control. Protection is evidenced by the retained integrity (intact band) of CNP/dsRNA complex compared to the degraded (smeared/disappeared) naked dsRNA on the gel.

$

Notes

This protocol simulates field-relevant stressors. The time points can be adjusted based on the expected application scenario.

{}

$

Sub-protocol 7: Oral Bioassay for dsRNA Efficacy via Double Sandwich Parafilm Method

**[PROTOCOL_STAGE=IN_VIVO_DELIVERY_FEEDING]**

$

Applicable when:

Administering dsRNA (naked or formulated) to sap-sucking insects like whiteflies through an artificial diet in a controlled feeding setup.

$

Purpose:

To deliver a precise concentration of dsRNA to adult whiteflies and assess its biological activity (mortality) over time.

$

Procedure:

1.  Diet Preparation: Prepare an artificial diet of 30% sucrose.

2.  Formulation Incorporation: Mix the optimized CNP/dsRNA complex stock (e.g., 200:1 ratio, final concentration 10 ng/μL) into the sucrose diet at the desired test concentrations (e.g., 2.5%, 5.0%, 10%, 15% v/v).

3.  Feeding Chamber Setup: Use a double sandwich parafilm method. Place the diet formulation between two stretched parafilm layers to create a sachet.

4.  Insect Introduction: Gently introduce 30 adult whiteflies (one-day-old) into the feeding chamber/bioassay cage containing the diet sachet.

5.  Maintenance: Conduct the assay aseptically to prevent microbial contamination. Maintain insects under standard rearing conditions.

6.  Mortality Scoring: Record whitefly mortality at 24, 48, and 72 hours post-feeding initiation.

7.  Replication: Repeat the entire experiment three times, with triplicates maintained for each concentration within each experiment.

$

Key materials and equipment:

- Artificial diet (30% sucrose)

- Optimized CNP/dsRNA formulation stock

- Parafilm

- Bioassay cages/chambers

- Aspirator for handling whiteflies

$

Controls_and_validation:

Control: Non-conjugated chitosan hydrogel mixed with artificial diet (vehicle control). Positive control could be a known lethal dsRNA. Statistical analysis (ANOVA, Tukey's HSD) is used to compare mortality among concentrations and time points.

$

Notes

Aseptic technique is crucial to avoid confounding mortality from microbial growth. The number of insects and replication scheme are designed for statistical robustness.

{}

$

Sub-protocol 8: Molecular Validation of Gene Knockdown via qRT-PCR

**[PROTOCOL_STAGE=QRT_PCR]**

$

Applicable when:

Quantifying the relative expression level of the target gene (EcR) in insects after exposure to dsRNA treatment, confirming RNAi mechanism at the molecular level.

$

Purpose:

To measure the transcript-level knockdown of the target gene, providing molecular evidence for the phenotypic effects observed in the bioassay.

$

Procedure:

1.  Sample Collection: After 72 hours of feeding on CNP/dsRNA diet, collect surviving whiteflies from each biological replicate.

2.  Total RNA Extraction: Extract total RNA from pooled whiteflies using a commercial kit (e.g., ISOLATE II RNA Mini Kit) following the manufacturer's protocol.

3.  cDNA Synthesis: Use 500 ng of total RNA for first-strand cDNA synthesis using a reverse transcription kit (e.g., RevertAid First Strand cDNA synthesis kit). Store cDNA at -20 °C.

4.  qRT-PCR Setup:

a.  Design primers for the target gene (EcR) and a stable reference gene (e.g., Elongation factor 1, EF1).

b.  Perform qPCR with an initial incubation at 95 °C for 1 min, followed by 40 cycles of: 95 °C for 5 s (denaturation) and 59 °C for 30 s (annealing/extension).

5.  Replication: Perform each experiment with three independent biological replicates (samples from independent treatments), with technical replicates.

6.  Data Analysis: Calculate relative expression levels using the 2-ΔΔCt method, comparing treated samples to the control group.

$

Key materials and equipment:

- RNA extraction kit (ISOLATE II RNA Mini Kit)

- cDNA synthesis kit (RevertAid)

- Real-time PCR system

- Primers for target (EcR) and reference (EF1) genes

$

Controls_and_validation:

Control group: Whiteflies fed on diet with non-conjugated chitosan hydrogel. Reference gene stability must be confirmed. The 2-ΔΔCt method normalizes target gene expression to the reference gene and the control group.

$

Notes

Sampling time (72h) is critical and based on the RNAi kinetics for the target. Primer specificity and reference gene stability are prerequisites for accurate quantification.